**Table 1.** Mean (standard deviation) of shear strength between acrylic resins before and after thermomechanical fatigue (MPa).

|  |  |  |
| --- | --- | --- |
| **Group** | **Before Fatigue** | **After Fatigue** |
| G1 - Conventional x Conventional | 16.76 (2.88) | 17.11 (3.82) |
| G2 - Conventional x 2.5% of AgVO3 | 17.52 (2.14) | 19.18 (2.47) |
| G3 - Conventional x 5% of AgVO3 | 19.83 (2.34) | 19.74 (3.93) |